# Product information
MATEX PREMIUM

# PO0134

Application

( Floor protection, for instance when painting, repairing or rebuilding

Why use MATEX

( Effective floor protection against paint drops

( Protects against scratches and pressure markings

( Easy to cut and use

( Superior wearing qualities

( Can be used several times

Product

( Needlepunched nonwoven textile from polyester fibres

( Homogenous structure

( Very fast and effective water absorption

( Laminated with strong anti-slip foil

Dimensions: 1x10 m, 1x25 m, 1x50 m, 2x50m

| Property | Standard | Unit | Value MD/CD |
| --- | --- | --- | --- |
| Weight | EN 29073-1 | g/m² | 160 ±20 |
| Thickness | EN ISO 9073-2 | Mm | 1,7 ±0,3 |
| Min. coating adhesion | EN ISO 2411 | N | 3 / 3 |
| Colour | White |
| Fibre composition | Polyester |
| Fibre bonding | Needlepunched |
| Treatment | Laminated with anti-slip foil |

MD: Machine direction / CD: Cross direction

Tolerance of width is ± 10 mm.

Laboratory tests are carried out on non-conditioned samples in non-conditioned testing 
environment. Testing conditions do not influence the results accuracy.

Fibertex reserves the right to change product data.